## Slide 1: Multi-Axis Crystal Spectrometer
Group 4
NCNR 2017 Summer School

## Slide 2: Outline
1.) How does MACS work?
2.) CuPzN and spinons
3.) Analysis and Results

## Slide 3: MACS
Highest flux cold source in the world
Incident Energy Range: 2.2-20 meV

## Slide 4: Double Analyzer/Detector Array
20 Detectors -- 8 degrees apart
Vertically focusing analyzers choose Kf
2 types of detectors for each channel, diffraction and spectroscopic
Diff. Detector
Spec. Detector

## Slide 5: Monochromator
45 cm
35 cm

## Slide 6: Crystal Information
CuPzN (Cu(C4H4N2)(NO3)2)
From heat capacity measurements: magnetic interactions are antiferromagnetic J=-0.9 meV
Pyrazine provides means of superexchange, so magnetic dynamics are expected to be highly one-dimensional
Small sample mass used (73mg), due to high flux on MACS this is possible
Image credit: H. Kuehne et al, Phys. Status Solidi B 247, 2010, DOI: 10.1002/pssb.200983077

## Slide 7: Spinons and Magnons
Spin flip splits into two spin ½ domain walls which propagate along the chain – these are spinons
Incident neutron causes a spin to flip
Classically:
Quantum:
Spinons sum as: and which results in a spin wave continuum
Image credits: S. Nagler et al, Phys. Rev. B 44, 1991, DOI: 10.1103/PhysRevB.44.12361

## Slide 8
Choosing parameters
E: – Best resolution (0.08 meV)
– He3 absorption, monitor count efficiency, fix , efficiency already known
(From heat capacity measurements J=-0.9 meV)
Q: ; steps 1
step 0.8
step
(h 0 0)
(0 k 0)
A3=90°
A3=0
ncnr summer school macs handout

## Slide 9
Filter: To eliminate higher order neutrons
Be – Cutoff at 5 meV (.404 nm)
~75% transmission below 5 meV
~20% transmission between 5 - 7 meV
BeO – Cutoff at 3.7 meV
~ 60% Transmission below 3.7meV
Be filter for both incident and scattered beam
– Better transmission and energy range
5 meV
7 meV
3.7 meV
Choosing parameters
Intensity decrease
http://www.iaea.org/inis/collection/NCLCollectionStore/_Public/41/046/41046596.pdf
https://ncnr.nist.gov/instruments/macs/Overview.html
3.7 meV E
I
FWHM
3.7 meV E
I
BeO filter

## Slide 10
Above, left: Symmetrized mapping of HK-plane showing no K-dependence along chains. Above, right: Spin-wave dispersion at T < 3K showing two-spinon continuum. J was found as .945(7) meV. Left: Movie of integrated K slicing through Temperature.
Spin-wave dispersion Dispersion

## Slide 11
Universal Behavior – 1D QCP
Independent of microscopic details of system
Universal energy/temperature scaling of collective response
Confirms that the system can be treated as 1D and near QCP
Above: (Bose factor * S(π,E)) plotted vs h*ω/2πkBT (Integrated over antiferromagnetic zone center parallel to chain direction)
Left: Integration cross section – (integrated over all measured K) for each temperature

## Slide 12: Acknowledgements
-Jose Rodriguez and Yiming Qiu (MACS Instrument Scientist)
-Kate Ross and Chris Stock
Special thanks to Yamali Hernandez and Alex Grutter for organizing NCNR Summer School
Additional thanks to all staff and scientists at NCNR